Fabrication Process # Photodiode

| Type Process Flow |  | Version v1 |  | Exported by Adish Gupta |  | Exported on Oct 30, 2026, 1:57 PM |
| --- | --- | --- | --- | --- | --- | --- |

Last saved  Oct 30, 2026, 10:28 AM

Open in FabuBlox  https://www.fabublox.com/designer/2cbbc24f-813f-4e72-a331-79439cbee9c8

# Substrate

| ### p-Si(100) with 300 nm Thermal SiO2 p-Si(100), 4", 1-10 ohm.cm, 300 nm thermal SiO2 (MTI), cleaved to ~2x2 cm dies Wafer Sizes 100mm - 4" Vendor MTI |  |
| --- | --- |

| Layer | Material | Thickness | Doping | Crystal Structure | Crystal Orientation |
| --- | --- | --- | --- | --- | --- |
| 1 | Silicon | 525 µm | p-type (B - Boron) | Single Crystal | <100> |
| 2 | SiO₂ | 300 nm | — | — | — |

# Process Flow

Section 1

## [A] PREP

| [A] PREP ### 1 Solvent clean Capability Type Chemical Clean Tool Name Wet Bench: Solvents Recipe Name - Process Parameters Cleaning Bath Composition: Acetone Ultra-Sonication: No Dry Method: N₂ blow dry Advanced Settings Keep Floating Structures: No Notes Process Intent: Cleans organic residues from the wafer surface prior to processing. Rationale: Sequential solvent clean: acetone > IPA > DI water rinse > N2 dry. |  |
| --- | --- |

| [A] PREP ### 2 RCA clean Capability Type RCA Clean Tool Name Wet Bench: RCA Recipe Name - Process Parameters SC 1 Constituents: SC-1 SC 2 Constituents: SC-2 Tool Parameters Dry Dry Method: N2 blow dry Advanced Settings Floating Structures Keep Floating Structures: No Notes Process Intent: Standard high-grade clean to remove trace organics, native oxide, and ionic/metallic contamination. Rationale: Per lab RCA references prior to photolithography and high-temperature processing. |  |
| --- | --- |

Section 2

## [B] MASK 1: ACTIVE WINDOWS

| [B] MASK 1: ACTIVE WINDOWS ### 3 Dehydration bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 300 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Dehydrates the wafer surface to promote resist adhesion. Rationale: ~120 °C for 5 min; HMDS primed if available. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 4 Spin S1813 Capability Type Spin-Coat Tool Name Spin Coater Recipe Name - Process Parameters Material Type: Positive Material: S1813 Film Thickness: 1.35 µm Spin Speed: 4000 rpm Spin Time: 50 secs Advanced Settings Fill Gaps: Yes Notes Process Intent: Coats positive photoresist S1813 for patterning active windows. Rationale: 4000 rpm for 50 s yields ~1.35 µm nominal thickness. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 5 Pre-exposure bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 115 °C Bake Time: 60 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Soft-bakes S1813 resist to remove casting solvents. Rationale: Hotplate pre-exposure bake at ~115 °C for 60 s. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 6 Expose Mask 1 Capability Type Direct-Write Lithography Tool Name litho-v1 Recipe Name - Process Parameters Laser Wavelength: 405 nm (h-line) Layer(s) to Expose: S1813 Pattern source: Manual Define Pattern: 1,4,1 Toggle start exposure region: Yes Advanced Settings Exposure Sidewall Angle: 5 ° Notes Process Intent: Exposes Mask 1 to define 500x500 µm active window, 200x200 µm pad area, marks, van der Pauw cross, and test diodes. Rationale: Patterned on litho-v1 DLP projector (405 nm LED) at 140 mJ/cm². |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 7 Develop Capability Type Develop Tool Name Wet Bench: MF-319 Recipe Name - Process Parameters Layer(s) to Develop: S1813 Developer: MF-319 Develop Time: 25 secs Advanced Settings Custom Undercut: No Notes Process Intent: Develops exposed S1813 photoresist. Rationale: MF-319 developer for 15-40 s (~30 s), followed by DI water rinse and N2 dry. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 8 Hard bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 600 secs Advanced Settings Hard-Bake All Resists: Yes Resist Image Reversal: No Notes Process Intent: Hardens resist mask prior to wet chemical oxide etching. Rationale: Hard bake at ~120 °C for 10 min. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 9 Etch oxide to Si Capability Type Chemical Etch Tool Name Wet Bench: BOE/DHF Recipe Name - Process Parameters Layer(s) to Etch: SiO₂ Two-Sided Etch: Yes Etch Bath Composition: BOE 6:1 Etch Depth: 300 nm Etch Time: 240 secs Advanced Settings Etch Mode: Isotropic Etch Define Etch Selectivity: No Out-of-plane Etch Buried Layers: No Keep Floating Structures: No Notes Process Intent: Etches 300 nm SiO2 thermally grown oxide down to bare silicon in opened active windows. Rationale: BOE wet etch for ~3-5 min (~4 min); visual endpoint indicated when bare silicon dewets. Leave backside uncoated by resist so the backside oxide is stripped simultaneously in this step for subsequent backside metallization. |  |
| --- | --- |

| [B] MASK 1: ACTIVE WINDOWS ### 10 Strip Resist Capability Type Chemical Clean Tool Name Wet Bench: PG Remover Recipe Name - Process Parameters Layer(s) to Remove: S1813 Cleaning Bath Composition: NMP Cleaning Time: 5 mins Cleaning Temperature: 60 °C Ultra-Sonication: No Dry Method: N2 blow dry Advanced Settings Keep Floating Structures: No |  |
| --- | --- |

Section 3

## [C] n+ EMITTER

| [C] n+ EMITTER ### 11 Dilute HF dip Capability Type Chemical Etch Tool Name Wet Bench: BOE/DHF Recipe Name - Process Parameters Layer(s) to Etch: SiO₂ Two-Sided Etch: No Etch Bath Composition: DHF 50:1 Etch Depth: 2 nm Etch Time: 10 secs Advanced Settings Etch Mode: Isotropic Etch Define Etch Selectivity: No Out-of-plane Etch Buried Layers: No Keep Floating Structures: No Notes Process Intent: Removes native oxide from active silicon windows prior to dopant application. Rationale: 10 s dilute HF (DHF 50:1) dip. |  |
| --- | --- |

| [C] n+ EMITTER ### 12 Spin P spin-on dopant Capability Type Spin-Coat Tool Name Spin Coater Recipe Name - Process Parameters Material Type: Dopant Dopant Species: P Material: Phosphorus Spin-On Dopant Film Thickness: 200 nm Spin Speed: 3000 rpm Spin Time: 45 secs Advanced Settings Fill Gaps: Yes Notes Process Intent: Applies phosphorus spin-on dopant to form shallow n+ emitter layer. Rationale: Spun per dopant recipe parameters. |  |
| --- | --- |

| [C] n+ EMITTER ### 13 Bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 165 °C Bake Time: 300 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Soft-bakes and dries spin-on dopant layer. Rationale: Hotplate bake at 150-175 °C (~165 °C). |  |
| --- | --- |

| [C] n+ EMITTER ### 14 Predeposition Capability Type Dopant Diffusion Tool Name Tube Furnace Recipe Name - Process Parameters Diffusion Target Layer(s): Silicon Gas-Source Diffusion: No Diffusion Distance: 300 nm Diffusion Temperature: 1100 °C Diffusion Time: 8 mins Advanced Settings Grow Thermal Surface Layer: No Notes Process Intent: Drives phosphorus dopant into exposed silicon active areas to form n+ emitter junction. Rationale: Tube furnace predeposition at 1100 °C for 5-10 min (~8 min). |  |
| --- | --- |

| [C] n+ EMITTER ### 15 Strip dopant glass Capability Type Chemical Etch Tool Name Wet Bench: BOE/DHF Recipe Name - Process Parameters Layer(s) to Etch: Phosphorus Spin-On Dopant Two-Sided Etch: No Etch Bath Composition: BOE 6:1 Etch Depth: 500 nm Etch Time: 60 secs Advanced Settings Etch Mode: Isotropic Etch Define Etch Selectivity: No Out-of-plane Etch Buried Layers: No Keep Floating Structures: No Notes Process Intent: Strips residual phosphosilicate dopant glass down to bare Si. Rationale: Brief BOE etch (60 s) to hydrophobic bare silicon surface. Note: This blanket dip also thins the field oxide from ~300 nm to ~200 nm, which remains sufficiently thick for subsequent Mask 2 and Mask 3 patterning. |  |
| --- | --- |

[C] n+ EMITTER ### M1 Measure R_sheet <GATE G1> Capability Type Metrology Tool Name Probe Station Recipe Name - Notes Process Intent: Measures sheet resistance (R_sheet) on van der Pauw cross structures as quality gate G1. Rationale: Confirms dopant drive-in and active layer sheet resistance before oxidation split.

Section 4

## [D] AR-OXIDE SPLIT

| [D] AR-OXIDE SPLIT ### 16 Dry O2 oxidation Capability Type Thermal Oxidation Tool Name Tube Furnace Recipe Name - Process Parameters Layer(s) to Consume: Silicon Two-Sided Growth: No Process Gases: O₂ Thermally Grown Material: SiO₂ Layer Thickness: 70 nm Growth Time: 20 mins Growth Temperature: 1100 °C Advanced Settings Consumption Ratio: 46 % Notes Process Intent: Thermally grows passivating anti-reflection (AR) oxide layer. Rationale: Dry O2 oxidation in furnace at 1100 °C; dies pulled at ~7 min (~40 nm), ~20 min (~70 nm), ~38 min (~100 nm), plus one bare-Si witness. |  |
| --- | --- |

[D] AR-OXIDE SPLIT ### M2 Measure oxide Capability Type Metrology Tool Name Ellipsometer Recipe Name - Notes Process Intent: Ellipsometer metrology of AR oxide thickness across split dies. Rationale: Confirms targets of ~40 nm / ~70 nm / ~100 nm AR oxide.

Section 5

## [E] MASK 2: CONTACT STRIPES

| [E] MASK 2: CONTACT STRIPES ### 17 Dehydration bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 300 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Dehydration bake before resist application. Rationale: 120 °C for 5 min. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 18 Spin S1813 Capability Type Spin-Coat Tool Name Spin Coater Recipe Name - Process Parameters Material Type: Positive Material: S1813 Film Thickness: 1.35 µm Spin Speed: 4000 rpm Spin Time: 50 secs Advanced Settings Fill Gaps: Yes Notes Process Intent: Coats S1813 positive resist for contact stripe mask. Rationale: 4000 rpm for 50 s. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 19 Pre-exposure bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 115 °C Bake Time: 60 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Soft-bakes S1813 resist. Rationale: 115 °C for 60 s. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 20 Expose Mask 2 Capability Type Direct-Write Lithography Tool Name litho-v1 Recipe Name - Process Parameters Laser Wavelength: 405 nm (h-line) Layer(s) to Expose: S1813 Pattern source: Manual Define Pattern: 2,1,2 Toggle start exposure region: Yes Advanced Settings Exposure Sidewall Angle: 5 ° Notes Process Intent: Exposes Mask 2 defining 10 µm contact opening stripes inside 30 µm fingers. Rationale: Patterned on litho-v1 DLP projector (405 nm LED), aligned to Mask 1 marks using XY + theta stage. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 21 Develop Capability Type Develop Tool Name Wet Bench: MF-319 Recipe Name - Process Parameters Layer(s) to Develop: S1813 Developer: MF-319 Develop Time: 25 secs Advanced Settings Custom Undercut: No Notes Process Intent: Develops exposed contact opening stripes in S1813 resist. Rationale: MF-319 developer for 15-40 s (~30 s), DI rinse, and N2 dry. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 22 Hard bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 600 secs Advanced Settings Hard-Bake All Resists: Yes Resist Image Reversal: No Notes Process Intent: Hardens resist mask prior to wet etching of contact stripes. Rationale: 120 °C for 10 min. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 23 Etch AR oxide Capability Type Chemical Etch Tool Name Wet Bench: BOE/DHF Recipe Name - Process Parameters Layer(s) to Etch: SiO₂ Two-Sided Etch: Yes Etch Bath Composition: BOE 6:1 Etch Depth: 100 nm Etch Time: 45 secs Advanced Settings Etch Mode: Isotropic Etch Define Etch Selectivity: No Out-of-plane Etch Buried Layers: No Keep Floating Structures: No Notes Process Intent: Etches opened contact stripes through AR oxide down to n+ emitter. Rationale: BOE etch time scaled by AR oxide thickness: ~25 s for 40 nm die, ~45 s for 70 nm die, and ~70 s for 100 nm die. Visual endpoint indicated when bare silicon contact stripes dewet. |  |
| --- | --- |

| [E] MASK 2: CONTACT STRIPES ### 24 Strip Resist Capability Type Chemical Clean Tool Name Wet Bench: PG Remover Recipe Name - Process Parameters Layer(s) to Remove: S1813 Cleaning Bath Composition: NMP Cleaning Time: 5 mins Cleaning Temperature: 60 °C Ultra-Sonication: No Dry Method: N2 blow dry Advanced Settings Keep Floating Structures: No |  |
| --- | --- |

Section 6

## [F] MASK 3: METAL BY SPUTTER + ETCH

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 25 Sputter Al Capability Type Sputter Tool Name sputter-v2 Recipe Name - Process Parameters Material: Aluminum Sputter Targets: Aluminum Process Gases: Argon Film Thickness: 300 nm Deposition Time: 1800 secs Tool Parameters Pumpdown Shutter Open: No Gas Stabilization Shutter Open: No Plasma Ignition Shutter Open: No Power Ramp-Up Shutter Open: No Target Conditioning Shutter Open: No Deposition Shutter Open: No Power Ramp-Down Shutter Open: No Purge Shutter Open: No Advanced Settings Conformal Deposition Controls Conformal Deposition: No Isotropy Ratio: 5% Maximum Deposition Angle: 85 ° Deposition Step Size: 0 nm Surface Interpolation: 0 nm Target Angle: 0 ° Maximum Gap to Fill: 0 nm Shadow Mask Shadow Mask: No Notes Process Intent: Blanket aluminium over the whole die for the contact fingers and pads. Rationale: DC magnetron sputtering in argon at about 0.001-0.01 mbar, 115 W, following the lab's sputter time. Sputtering gives good step coverage over the field-oxide step. 300 nm is a design target; the true rate is not documented and will be calibrated with a profilometer. Pre-sputter a few minutes behind a shutter or dummy piece to clean the target. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 26 Dehydration bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 300 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Removes adsorbed water from the Al surface before the resist. Rationale: 120 °C for 5 min, then cool to room temperature. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 27 Spin S1813 Capability Type Spin-Coat Tool Name Spin Coater Recipe Name - Process Parameters Material Type: Positive Material: S1813 Film Thickness: 1.35 µm Spin Speed: 4000 rpm Spin Time: 50 secs Advanced Settings Fill Gaps: Yes Notes Process Intent: Coats S1813 positive photoresist as etch mask for Aluminum patterning. Rationale: About 1.35 µm positive photoresist as the etch mask (4000 rpm, 50 s). |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 28 Pre-exposure bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 115 °C Bake Time: 60 secs Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Soft-bakes S1813 photoresist before exposure. Rationale: 115 °C for 60 s. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 29 Expose Mask 3 Capability Type Direct-Write Lithography Tool Name litho-v1 Recipe Name - Process Parameters Laser Wavelength: 405 nm (h-line) Layer(s) to Expose: S1813 Pattern source: Manual Define Pattern: 2,1,2 Toggle start exposure region: No Advanced Settings Exposure Sidewall Angle: 5 ° Notes Process Intent: Define the Al fingers, bus bar and pads, aligned to Mask 2. Rationale: S1813 is a positive resist, so the Al to keep must stay unexposed. Dose may need a small trim because Al is reflective. Tool is a DLP projector with a 405 nm LED, not a laser. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 30 Develop Capability Type Develop Tool Name Wet Bench: MF-319 Recipe Name - Process Parameters Layer(s) to Develop: S1813 Developer: MF-319 Develop Time: 30 secs Advanced Settings Custom Undercut: No Notes Process Intent: Develops exposed S1813 photoresist. Rationale: MF-319 for 30 s. Then DI water rinse and N2 dry. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 31 Hard bake Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 120 °C Bake Time: 120 secs Advanced Settings Hard-Bake All Resists: Yes Resist Image Reversal: No Notes Process Intent: Hardens the resist so the aqueous acid etch does not lift it. Rationale: 120 °C for 2 min. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 32 Etch Al Capability Type Chemical Etch Tool Name Wet Bench: Al etchant Recipe Name - Process Parameters Layer(s) to Etch: Aluminum Two-Sided Etch: No Etch Bath Composition: Al etchant (H3PO4 : HNO3 : H2O = 40 : 7 : 7 by volume) Etch Depth: 300 nm Etch Time: 300 secs Advanced Settings Etch Mode: Isotropic Etch Define Etch Selectivity: No Out-of-plane Etch Buried Layers: No Keep Floating Structures: No Notes Process Intent: Remove the Al outside the finger, bus-bar and pad pattern. Rationale: Phosphoric/nitric acid mix, endpoint by eye plus about 30 s over-etch; time and temperature are calibrated on a dummy die. Isotropic undercut is about the film thickness (0.3 um), small compared with the 30 um fingers. Keep nitric acid away from acetone, IPA and organic solvents; fume hood, acid gloves. |  |
| --- | --- |

| [F] MASK 3: METAL BY SPUTTER + ETCH ### 33 Strip resist Capability Type Chemical Clean Tool Name Wet Bench: NMP Recipe Name - Process Parameters Layer(s) to Remove: S1813 Cleaning Bath Composition: NMP Cleaning Time: 5 mins Cleaning Temperature: 60 °C Ultra-Sonication: No Dry Method: N₂ blow dry Advanced Settings Keep Floating Structures: No Notes Process Intent: Completely removes S1813 etch mask resist. Rationale: NMP bath at 60 °C for 5 min. Then IPA rinse, DI water rinse, N2 dry. |  |
| --- | --- |

Section 7

## [G] BACKSIDE + SINTER

| [G] BACKSIDE + SINTER ### 34 Backside contact Capability Type Custom Step Tool Name - Recipe Name - Process Parameters Comment: Apply ~200 nm evaporated Al, silver epoxy, or indium paste (backside oxide stripped earlier during Steps 9 and 23 BOE etches). Notes Scratch the backside lightly with a diamond scribe before applying silver epoxy or indium, because phosphorus vapour during predeposition (step 14) can form a thin n-type skin there. Process Intent: Applies ohmic backside contact metallization. Rationale: Backside oxide was stripped earlier during Steps 9 and 23 BOE etches. Apply ~200 nm evaporated Al, silver epoxy, or indium paste to form backside substrate contact without exposing front-side Al to BOE. |  |
| --- | --- |

| [G] BACKSIDE + SINTER ### 35 Sinter Capability Type Bake Tool Name Hot Plate Recipe Name - Process Parameters Bake Temperature: 380 °C Bake Time: 10 mins Advanced Settings Hard-Bake All Resists: No Resist Image Reversal: No Notes Process Intent: Sinters the Al contacts to form low-resistance ohmic contacts. Rationale: 380 °C, 10 min on a hotplate in air. Kept at or below 400 °C to avoid Al spiking through the shallow junction. |  |
| --- | --- |

Section 8

## [H] TEST

[H] TEST ### M3 Dark I-V <GATE G2> Capability Type Metrology Tool Name Probe Station Recipe Name - Notes Process Intent: Measures dark I-V characteristics as quality gate G2. Rationale: Confirms diode rectification >= 10^3 between +/-1 V.

[H] TEST ### M4 Photocurrent <GATE G3/G4> Capability Type Metrology Tool Name Probe Station Recipe Name - Notes Process Intent: Measures photocurrent response on litho-v1 stage under 405 nm LED illumination as quality gate G3/G4. Rationale: Quantifies on/off response difference vs AR oxide thickness split (40/70/100 nm) and vs finger pitch.

[H] TEST ### M5 Linearity Capability Type Metrology Tool Name Probe Station Recipe Name - Notes Process Intent: Evaluates photocurrent linearity over optical power. Rationale: Measures photocurrent (I_ph) versus LED driving current.

[H] TEST ### M6 Calibration Capability Type Metrology Tool Name Probe Station Recipe Name - Notes Process Intent: Calibrates photodiode responsivity and external quantum efficiency (EQE). Rationale: Benchmarks against a calibrated commercial silicon photodiode standard.