Substrate, Tools & Materials # Photodiode Requirements

| Type Process Flow |  | Version v1 |  | Exported by Adish Gupta |  | Exported on Oct 30, 2026, 8:44 AM |
| --- | --- | --- | --- | --- | --- | --- |

Last saved  Oct 29, 2026, 8:12 PM

Open in FabuBlox  https://www.fabublox.com/designer/2cbbc24f-813f-4e72-a331-79439cbee9c8

# Required Substrate

### p-Si(100) with 300 nm Thermal SiO2

p-Si(100), 4", 1-10 ohm.cm, 300 nm thermal SiO2 (MTI), cleaved to ~2x2 cm dies

Wafer Sizes	100mm - 4"

Vendor	MTI

| Layer | Material | Thickness | Doping | Crystal Structure | Crystal Orientation |
| --- | --- | --- | --- | --- | --- |
| 1 | Silicon | 525 µm | p-type (B - Boron) | Single Crystal | <100> |
| 2 | SiO₂ | 300 nm | — | — | — |

# Required Tools

| Tool Name | Capability Type | Used in |
| --- | --- | --- |
| Wet Bench: Solvents | Chemical Clean | Step 1 |
| Wet Bench: RCA | RCA Clean | Step 2 |
| Hot Plate | Bake | Steps 3, 5, 8, 13, 17, 19, 22, 25, 27, 29, 35 |
| Spin Coater | Spin-Coat | Steps 4, 12, 18, 26, 28 |
| litho-v1 | Direct-Write Lithography | Steps 6, 20, 30 |
| Wet Bench: MF-319 | Develop | Steps 7, 21, 31 |
| Wet Bench: BOE/DHF | Chemical Etch | Steps 9, 11, 15, 23 |
| Wet Bench: PG Remover | Chemical Clean | Steps 10, 24 |
|  | Lift-Off | Step 33 |
| Tube Furnace | Dopant Diffusion | Step 14 |
|  | Thermal Oxidation | Step 16 |
| Probe Station | Metrology | Steps M1, M3, M4, M5, M6 |
| Ellipsometer | Metrology | Step M2 |
| thermal-evaporator-v1 | Thermal Evaporation | Step 32 |
| - | Custom Step | Step 34 |

# Required Materials

Source: the step deposits or consumes the material.   Target: the step acts on material already there, such as etching it.

| Material | Composition | Used in |
| --- | --- | --- |
| Silicon | Si | Source: Substrate Target: Steps 14, 16 |
| SiO₂ | SiO₂ | Source: Substrate, Step 16 Target: Steps 9, 11, 23 |
| S1813 | 75wt% PGMEA, 20wt% Cresol Novolac Resin, 5wt% DNQ Photoactive Compound | Source: Steps 4, 18, 28 Target: Steps 6, 7, 10, 20, 21, 24, 30, 31 |
| Phosphorus Spin-On Dopant | TEOS:H₂O:H₃PO₄ (1:4:0.1) in IPA | Source: Step 12 Target: Step 15 |
| LOR 3A | 6wt% PMGI, 94wt% Cyclopentanone | Source: Step 26 |
| Aluminum | Al | Source: Step 32 |